# Multi-layer conductive spray coating

THREE-LAYER CONDUCTIVE COATING FOR RF SHIELDING

Lightweight 50 MHz RF Isolation Solution for Carbon Fiber Housing

| Document ID | RF-SHIELD-3L-001 |
| --- | --- |
| Revision | Rev. A — Draft for Review |
| Date | 2026-07-10 |
| Classification | Engineering Technical Document |

# 1. EXECUTIVE SUMMARY

This document presents a three-layer conductive coating solution designed to provide >40 dB RF isolation at 50 MHz for a lightweight carbon fiber sensor housing. The coating system—comprising alternating conductive (Cu/Ag-loaded paint) and dielectric layers—is applied to the interior surface via air atomization spray, achieving a total thickness under 100 µm and a mass budget below 0.3 kg. This approach eliminates the 1.5–3 kg mass penalty associated with continuous metal liners while preserving the housing's IP54 thermal management baseline and structural integrity.

# 2. PROBLEM STATEMENT

The existing carbon fiber composite housing provides inadequate electromagnetic shielding at 50 MHz, the operating frequency of the Ground-Penetrating Radar (GPR) system. Unattenuated RF leakage penetrates the enclosure and couples into sensitive subsystems:

MCT (Mercury Cadmium Telluride) Detector — susceptible to noise-induced drift and reduced signal-to-noise ratio.

Geophone ADC — analog-to-digital conversion accuracy degraded by conducted and radiated EMI.

Target isolation requirement: >40 dB to ensure operational integrity in high-RF environments.

Traditional solutions (e.g., continuous aluminum or copper liners) add 1.5–3 kg of mass, compromise thermal venting, and increase manufacturing complexity. A lightweight, conformal alternative is required.

# 3. SOLUTION ARCHITECTURE

## 3.1 Three-Layer Conductive Coating Structure

The proposed solution applies a multi-layer stack to the interior surface of the carbon fiber housing. Each layer is separated by a dielectric spacer, creating multiple impedance mismatch interfaces that reflect and absorb incident RF energy through a combination of skin-effect attenuation and wave interference.

| Layer | Material | Thickness | Function |
| --- | --- | --- | --- |
| Substrate | Carbon Fiber Composite | — | Structural housing, interior surface |
| Conductive Layer 1 | Cu/Ag-loaded conductive paint | 15–25 µm | Primary reflection / skin-effect attenuation |
| Dielectric Spacer 1 | Polymer-based dielectric | 5–10 µm | Impedance mismatch interface |
| Conductive Layer 2 | Cu/Ag-loaded conductive paint | 15–25 µm | Secondary reflection / absorption |
| Dielectric Spacer 2 | Polymer-based dielectric | 5–10 µm | Impedance mismatch interface |
| Conductive Layer 3 | Cu/Ag-loaded conductive paint | 15–25 µm | Tertiary reflection / final attenuation barrier |

Total stack thickness: <100 µm | Total added mass: <0.3 kg

## 3.2 RF Shielding Mechanism

At 50 MHz, the wavelength in free space is approximately 6 m. Inside the conductive coating, the skin depth of copper/silver-loaded paint (effective conductivity ~10⁴–10⁵ S/m) is on the order of tens of micrometers. The three-layer stack operates via two complementary mechanisms:

Reflection Loss: Each conductive–dielectric interface creates an impedance discontinuity (Z₀ ≈ 377 Ω in air vs. Z_metal ≈ 0.01–0.1 Ω). At 50 MHz, the reflection coefficient Γ at each boundary is >0.999, causing multiple internal reflections that trap RF energy within the coating stack.

Absorption Loss: Conductive layers dissipate penetrating RF energy as ohmic heat via the skin effect. With three sequential layers, cumulative absorption exceeds the threshold required for >40 dB isolation across the operational bandwidth.

# 4. APPLICATION PROCESS

## 4.1 Surface Preparation

Adhesion and long-term durability of the coating depend critically on substrate preparation. The following steps are performed prior to spray application:

Step 1: Cleaning & Degreasing — Remove mold release agents, oils, and particulate contaminants using isopropyl alcohol or approved solvent wipe.

Step 2: Light Abrasion — Gently abrade the interior carbon fiber surface with fine-grit abrasive pad (e.g., P320–P400) to increase surface energy and mechanical bonding sites. Vacuum debris post-abrasion.

Step 3: Masking — Protect sensor mount zones, thermal vent paths, and quick-swap interface areas with precision-cut masking tape or removable plugs.

## 4.2 Spray Application (Air Atomization)

The conductive paint is applied using a conventional air-atomization spray gun (HVLP or compliant) under controlled environmental conditions (temperature 20–25 °C, relative humidity 40–60%). Process parameters:

| Parameter | Specification |
| --- | --- |
| Gun Distance | 150–200 mm from substrate surface |
| Air Pressure | 1.5–2.5 bar (regulated at gun inlet) |
| Fluid Flow Rate | 150–250 mL/min |
| Layer Build Rate | 5–8 µm per pass; flash-off 5–10 min between passes |
| Dielectric Spacer Application | Spray-applied polymer spacer or pre-cut film lamination; thickness verified by eddy-current or micrometer gauge |

Cure cycle: To be validated per paint manufacturer datasheet (typically 24 h ambient or 60 min at 80 °C).

# 5. DESIGN CONSTRAINTS & CLEARANCES

The coating is applied exclusively to interior surfaces and is engineered to preserve all functional clearances:

• Sensor Mount Zones: Left clear of coating to ensure electrical and thermal interface integrity with MCT detector and geophone ADC modules.

• Thermal Vent Paths: Unobstructed to maintain convective cooling performance and IP54-rated thermal management baseline.

• Quick-Swap Interface: Exposed for tool-less module exchange; coating terminated with a 2 mm margin from interface edges.

• Mass Budget: <0.3 kg total added mass (vs. 1.5–3 kg for metal liner alternative).

• Thermal Mass: Negligible increase; coating specific heat capacity and thickness do not alter thermal time constants.

# 6. PERFORMANCE SPECIFICATIONS

| Parameter | Target | Verification Method |
| --- | --- | --- |
| RF Isolation | >40 dB @ 50 MHz | MIL-STD-285 / IEEE 299 shielding effectiveness test |
| Total Coating Thickness | <100 µm | Eddy-current or cross-sectional microscopy |
| Added Mass | <0.3 kg | Precision balance (±1 g resolution) |
| Adhesion Strength | >5B (ASTM D3359) or equivalent | Cross-hatch tape test |
| Operating Temperature | -20 °C to +60 °C | Environmental chamber cycling |

# 7. VALIDATION & TEST PLAN

## 7.1 Environmental Durability

Long-term shielding stability under operational and storage conditions requires accelerated life testing. The following test matrix is proposed:

| Test | Condition | Duration | Acceptance Criteria |
| --- | --- | --- | --- |
| Vibration Durability | 50–400 Hz, 5–20 g RMS random | Per axis, 8 h minimum | No cracking, delamination, or >3 dB shielding degradation |
| Tropical Humidity | 40 °C / 95% RH | 500 h (IEC 60068-2-78) | No corrosion, blistering, or >3 dB shielding degradation |
| Thermal Cycling | -20 °C ↔ +60 °C | 100 cycles | No cracking or adhesion loss; shielding stable |

## 7.2 Shielding Effectiveness Verification

Shielding effectiveness (SE) shall be measured per MIL-STD-285 or IEEE 299 using a dual-chamber method. A 50 MHz CW signal is injected into the source chamber; field strength is measured in the receive chamber with and without the coated housing panel installed. SE is calculated as:

SE (dB) = 20 log₁₀(E_without / E_with)

# 8. RISK ASSESSMENT

| Risk | Likelihood | Impact | Mitigation |
| --- | --- | --- | --- |
| Adhesion failure under vibration | Medium | High | Optimized surface prep + primer layer; qualification vibration test |
| Humidity-induced corrosion of conductive layer | Low | Medium | Use Ag-loaded paint (more corrosion-resistant than Cu); conformal coat option |
| Thickness non-uniformity affecting SE | Medium | Medium | Automated spray robot with real-time thickness monitoring |
| Dielectric spacer delamination | Low | High | Validated cure cycle; peel strength testing per ASTM D1876 |

# 9. CROSS-DOMAIN INTEGRATION

This solution bridges materials science, electromagnetics, and manufacturing engineering:

Materials Science: Selection of conductive filler (Cu vs. Ag) balances cost, conductivity, and corrosion resistance; dielectric spacer chemistry optimized for adhesion to both carbon fiber and metal-filled paint.

Electromagnetics: Layer thickness and conductivity tuned to maximize reflection and absorption at 50 MHz via transmission-line modeling (e.g., CST Studio Suite, ANSYS HFSS).

Manufacturing Engineering: Air atomization spray process scaled from aerospace and automotive EMI coating practices; masking and fixturing designed for batch production.

Systems Engineering: Mass, thermal, and structural budgets reconciled with RF performance requirements; traceability matrix maintained from requirement to verification.

# 10. REFERENCES

[1] Conductive Coating Spraying Method Based on Lightweight Product — Internal Process Reference Document.

[2] MIL-STD-285, 'Military Standard: Attenuation Measurements for Enclosures, Electromagnetic Shielding, for Electronic Test Purposes.'

[3] IEEE Std 299-2006, 'IEEE Standard Method for Measuring the Effectiveness of Electromagnetic Shielding Enclosures.'

[4] ASTM D3359, 'Standard Test Method for Measuring Adhesion by Tape Test.'

[5] IEC 60068-2-78, 'Environmental Testing — Part 2-78: Tests — Test Cab: Damp Heat, Steady State.'

[6] Schelkunoff, S.A. 'Electromagnetic Waves.' D. Van Nostrand Company, 1943. (Shielding theory foundation)

# 11. APPENDIX: TECHNICAL CONTRACTIONS & SEGMENTATION

## 11.1 Technical Contradictions Resolved

• RF Isolation vs. Mass: Traditional metal liners provide isolation but violate the mass budget. The segmented multi-layer coating achieves comparable isolation with <10% of the liner mass.

• Conductivity vs. Thermal Mass: High-conductivity metals add thermal mass. The thin-paint approach adds negligible thermal capacitance while providing sufficient conductivity for skin-effect attenuation.

• Coverage vs. Functional Clearances: Full interior coverage would obstruct mounts and vents. Segmented masking preserves critical zones while coating all RF-leakage pathways.

## 11.2 Segmentation Strategy

The coating is segmented into functional zones to optimize manufacturability and serviceability:

Primary Shield Zone: Covers all interior walls subject to direct RF illumination; receives full 3-layer stack.

Transition Zone: 2–3 mm margin around sensor mounts and vents; receives 1-layer conductive ground plane to maintain electrical continuity without obstructing function.

Exclusion Zone: Quick-swap interface and external connector faces; uncoated to preserve mechanical tolerances and mating surfaces.

# DOCUMENT CONTROL

| Prepared By | Engineering Team |
| --- | --- |
| Reviewed By | RF / EMI Specialist |
| Approved By | Chief Engineer |
| Distribution | Restricted — Engineering & QA |
| Next Review Date | 2026-10-10 (90 days from issue) |