PHASE-CHANGE THERMAL BUFFER LAYER

Transient Heat Peak Absorption in Sealed Carbon Fiber Pod

Saturday, July 11, 2026

| Document ID | THERM-PCM-001 |
| --- | --- |
| Revision | Rev. A — Draft for Review |
| Date | 2026-07-11 |
| Classification | Engineering Technical Document |

# 1. EXECUTIVE SUMMARY

This document presents a phase-change material (PCM) thermal buffer layer solution for transient heat peak management in a sealed carbon fiber pod. A 3–5 mm honeycomb-structured PCM layer (~0.3–0.5 kg, melting point 35–40 °C, latent heat ~150–200 kJ/kg) is embedded inside the carbon fiber shell, bonded to aluminum structural ribs and coated with carbon nanotubes (CNT) for enhanced thermal conductivity (5–8 W/m·K). During high-power sensor operations (QCL spectroscopy, GPR pulses), the PCM melts and absorbs 60–80 kJ of transient thermal load, preventing TEC saturation and temperature spikes; during flight idle or ground periods, the PCM solidifies and passively releases stored heat to the shell exterior via conduction. This time-separated heat storage and rejection mechanism maintains QCL/MinION within operating limits without opening the sealed IP54 enclosure, adds <0.5 kg to pod mass, requires no active cooling hardware or power budget increase, and integrates with existing structural ribs for <5 min field serviceability.

# 2. PROBLEM STATEMENT

The sealed carbon fiber pod experiences transient thermal peaks during high-power sensor operations, creating critical thermal management deficiencies:

Heat spikes from high-power operation — QCL spectroscopy and GPR pulses generate rapid, high-magnitude thermal transients that exceed steady-state TEC capacity.

TEC saturation risk — thermoelectric coolers rated for 15–20 W continuous heat pumping cannot absorb peak loads of 40–60 W during burst operations.

Temperature overshoot — transient peaks drive QCL and MinION junction temperatures beyond operating limits (>45 °C and >40 °C respectively), causing performance degradation.

Sealed enclosure constraint — the IP54-rated pod cannot be opened for active cooling or ventilation during operation.

Power budget limitation — no additional power available for active cooling hardware (fans, pumps, secondary TECs).

Mass budget limitation — active cooling hardware would violate the ≤12 kg pod mass budget.

Goal: Absorb 60–80 kJ of transient thermal energy during peak operations and release it during idle periods, maintaining QCL/MinION within operating limits without active cooling, power increase, or seal breach.

# 3. SOLUTION ARCHITECTURE

## 3.1 PCM Layer Configuration

The PCM thermal buffer is integrated into the pod wall structure as a conformal layer, leveraging existing structural elements for thermal coupling and mechanical support:

| Component | Material / Geometry | Dimensions | Function |
| --- | --- | --- | --- |
| PCM Matrix | Organic PCM (e.g., paraffin wax RT35 or salt hydrate) | 3–5 mm thick honeycomb | Latent heat storage: absorbs/releases 60–80 kJ per cycle |
| Honeycomb Structure | Aluminum or polymer honeycomb core | Cell size 3–6 mm, wall thickness 0.05 mm | Contains PCM, prevents leakage during phase change, maintains shape |
| CNT Coating | Multi-walled carbon nanotubes (MWCNT) in epoxy binder | 50–100 µm coating thickness | Enhances thermal conductivity from ~0.2 to 5–8 W/m·K |
| Bond Layer | Thermal interface material (TIM) or structural epoxy | 0.1–0.2 mm | Mechanical bonding to aluminum ribs; thermal coupling to heat sources |
| Aluminum Ribs | 6061-T6 aluminum structural members | Existing pod structure | Heat spreaders: conduct heat from QCL/MinION/TEC to PCM layer |
| Carbon Fiber Shell | CFRP composite | 2–3 mm wall thickness | Structural enclosure; radiates stored heat to ambient during idle |

## 3.2 Time-Separated Thermal Action Path

The PCM buffer operates through a time-separated cycle that decouples heat generation from heat rejection:

Phase 1: High-Power Operation (Heat Absorption): During QCL spectroscopy and GPR pulse bursts, heat generation exceeds TEC capacity. Excess heat conducts through aluminum ribs to the PCM layer. As the PCM temperature reaches its melting point (35–40 °C), it begins to melt, absorbing latent heat at nearly constant temperature. A 0.3–0.5 kg PCM layer with L ≈ 150–200 kJ/kg can absorb 60–80 kJ, equivalent to ~15–20 minutes of 40–60 W peak load beyond TEC capacity. The QCL/MinION junction temperature is clamped at ~40 °C during melting.

Phase 2: Cruise / Idle (Heat Storage): During flight cruise or low-power idle, heat generation drops below TEC capacity. The TEC continues to pump heat from the electronics cold plate, but the PCM remains partially or fully molten, storing absorbed energy. The sealed enclosure prevents heat loss to ambient, maintaining the stored energy in the PCM.

Phase 3: Ground / Low Load (Heat Rejection): During ground idle or shutdown, the TEC is off and electronics generate minimal heat. The molten PCM begins to solidify, releasing stored latent heat to the carbon fiber shell via conduction through the CNT coating and aluminum ribs. The shell radiates and convects heat to ambient, completing the thermal cycle. Solidification temperature is ~35–38 °C (supercooling minimized by nucleation agents in PCM formulation).

## 3.3 Thermal Profile Flattening Over Mission Cycle

The PCM buffer transforms a spiky thermal profile into a flattened profile by time-shifting heat rejection:

Without PCM: Peak load → immediate temperature spike → TEC saturation → QCL/MinION exceed limits → mission abort or performance degradation.

With PCM: Peak load → PCM melts → temperature clamped at ~40 °C → heat stored → idle period → PCM solidifies → heat released to shell → temperature remains within limits throughout cycle.

Effective Heat Capacity: The apparent heat capacity of the PCM layer during melting is: C_eff = m × L / ΔT. For m = 0.4 kg, L = 175 kJ/kg, ΔT = 5 °C (35–40 °C range): C_eff = 0.4 × 175,000 / 5 = 14,000 J/K. This is equivalent to ~3.5 kg of aluminum or ~14 kg of water in sensible heat capacity, demonstrating the mass efficiency of latent heat storage.

# 4. DESIGN DETAILS

## 4.1 PCM Material Selection

The PCM is selected based on melting point, latent heat, thermal stability, and compatibility with the pod environment:

| Parameter | Specification |
| --- | --- |
| PCM Type | Organic: Paraffin wax RT35 (Rubitherm) or RT40; Inorganic: Salt hydrate CaCl₂·6H₂O (with nucleation agents) |
| Melting Point | 35–40 °C (selected to be 5–10 °C above maximum ambient, ensuring melting only from internal heat load) |
| Latent Heat | ~150–200 kJ/kg (organic paraffin) or ~170 kJ/kg (salt hydrate) |
| Density (Solid) | ~800–900 kg/m³ (paraffin); ~1700 kg/m³ (salt hydrate) |
| Thermal Conductivity (Bulk) | ~0.2 W/m·K (paraffin); ~1.0 W/m·K (salt hydrate) — enhanced to 5–8 W/m·K via CNT coating |
| Volume Change | <10% (paraffin); ~5% (salt hydrate) — accommodated by honeycomb cell expansion |
| Cycling Stability | >1000 cycles without significant degradation (verified by DSC testing) |
| Toxicity / Safety | Non-toxic, non-flammable, compatible with aluminum and carbon fiber |

## 4.2 CNT Thermal Enhancement Coating

The carbon nanotube coating addresses the inherently low thermal conductivity of organic PCMs:

CNT Type: Multi-walled carbon nanotubes (MWCNT), diameter 10–30 nm, length 5–20 µm, purity >95%.

Matrix: Epoxy resin (low viscosity) with 5–10 wt% MWCNT loading, achieving percolation threshold for conductive network.

Coating Method: Spray coating or dip coating onto honeycomb cell walls, followed by thermal cure at 80 °C.

Thermal Conductivity Enhancement: Bulk PCM conductivity ~0.2 W/m·K → CNT-coated layer 5–8 W/m·K (25–40× improvement). This ensures rapid heat transfer between aluminum ribs and PCM during both melting and solidification.

Mechanical Properties: CNT coating adds negligible mass (<0.02 kg) and maintains flexibility to accommodate PCM volume change.

## 4.3 Honeycomb Containment Structure

The honeycomb structure contains the PCM during phase change, preventing leakage and maintaining dimensional stability:

| Parameter | Specification |
| --- | --- |
| Core Material | Aluminum 5052-H39 or Nomex aramid paper (depending on mass budget) |
| Cell Geometry | Hexagonal cells, 3–6 mm cell size, 3–5 mm total core thickness |
| Cell Wall Thickness | 0.05 mm (aluminum) or 0.1 mm (Nomex) |
| PCM Fill Factor | >90% of honeycomb cell volume filled with PCM |
| Sealing | Aluminum foil or polymer film bonded to honeycomb faces to contain liquid PCM |
| Mass | ~0.1 kg (honeycomb) + 0.3–0.5 kg (PCM) = ~0.4–0.6 kg total buffer layer |

## 4.4 Thermal Analysis & Sizing

The PCM layer is sized to absorb the expected transient heat load over the mission cycle:

Heat Load Characterization: QCL spectroscopy: 25–35 W peak, 10–15 min bursts. GPR pulses: 15–25 W peak, 5–10 min bursts. TEC baseline: 15–20 W continuous. Net transient excess = (25–35 + 15–25) – 15–20 = 25–40 W during peak operations.

Energy Storage Requirement: Typical mission cycle: 2–3 peak bursts per hour, each 10–15 min. Total transient energy per cycle = 25–40 W × 600–900 s = 15,000–36,000 J = 15–36 kJ. Design margin (2×): 60–80 kJ storage capacity.

PCM Mass Calculation: m = E_storage / L = 70,000 J / 175,000 J/kg = 0.40 kg. With honeycomb containment: total buffer mass ≈ 0.5 kg.

Melting Time: t_melt = (m × L) / Q_excess = 70,000 J / 35 W = 2000 s ≈ 33 min. This exceeds typical burst duration (10–15 min), ensuring the PCM does not fully melt during a single burst and can handle multiple bursts per cycle.

Solidification Time: t_solid = (m × L) / Q_rejection. During ground idle, heat rejection to ambient via shell: Q_rejection ≈ hAΔT + εσA(T_s⁴ – T_a⁴). With h ≈ 10 W/m²·K, A ≈ 0.4 m², ΔT ≈ 10 °C: Q_conv ≈ 40 W. Radiation: Q_rad ≈ 15 W. Total Q_rejection ≈ 55 W. t_solid ≈ 70,000 / 55 ≈ 1270 s ≈ 21 min. Ground idle period typically >30 min, ensuring full recharge.

# 5. INTEGRATION & FIELD SERVICEABILITY

## 5.1 Structural Integration

The PCM buffer layer integrates with existing pod structural elements without major redesign:

Rib Bonding: The honeycomb-PCM panel is bonded to aluminum structural ribs using thermally conductive epoxy (k > 2 W/m·K). The ribs serve as heat spreaders, conducting heat from QCL/MinION/TEC mounting plates to the PCM layer.

Shell Interface: The outer face of the honeycomb panel is bonded to the inner surface of the carbon fiber shell. During solidification, heat conducts through the shell to ambient. The CNT coating on the shell-facing side enhances this heat rejection path.

Modular Panel Design: The PCM layer is manufactured as curved panels matching the pod interior geometry. Panels are segmented into 4–6 sections for handling and replacement. Each panel has alignment pins and quick-release fasteners.

## 5.2 Field Service Procedure (<5 min target)

The modular panel design enables rapid field replacement:

Step 1: Access Panel Removal
Open the pod quick-access panel (hinged or removable). The PCM buffer panels are visible on the interior shell surface.

Step 2: Release Fasteners
Loosen 4–6 quarter-turn fasteners per PCM panel (no tools required).

Step 3: Remove Old Panel
Slide the panel out along alignment rails. The panel is lightweight (~0.1 kg per section) and manageable by one person.

Step 4: Install New Panel
Slide replacement panel into position. Alignment pins ensure correct orientation.

Step 5: Secure Fasteners
Hand-tighten quarter-turn fasteners. Close access panel. Total time: <5 min.

# 6. PERFORMANCE SPECIFICATIONS

| Parameter | Target | Verification Method |
| --- | --- | --- |
| Heat Storage Capacity | 60–80 kJ per cycle | Calorimetry (DSC) + thermal cycling test with known heat load |
| PCM Thickness | 3–5 mm | CMM measurement of prototype panels |
| PCM Mass | ~0.3–0.5 kg | Precision balance |
| Thermal Conductivity (CNT-coated) | 5–8 W/m·K | Laser flash analysis (ASTM E1461) or guarded hot plate |
| Melting Point | 35–40 °C | Differential scanning calorimetry (DSC) per ASTM E794 |
| Temperature Clamping | QCL/MinION <45 °C during peak load | Thermocouple array during simulated mission cycle |
| Cycling Stability | >1000 cycles without >10% degradation | Accelerated thermal cycling (DSC before/after) |
| Field Service Time | <5 min (panel replacement) | Stopwatch, trained operator, 10 trials |
| Added Mass | <0.5 kg | Precision balance |
| Power Consumption | Zero (passive) | Power meter verification |

# 7. VALIDATION & TEST PLAN

## 7.1 PCM Material Characterization

PCM properties shall be validated through laboratory testing:

DSC Analysis: Measure melting point, latent heat, and specific heat capacity using differential scanning calorimetry (ASTM E794). Verify melting point is 35–40 °C and latent heat is 150–200 kJ/kg. Test sample: 10 mg, heating rate 5 °C/min.

Thermal Conductivity: Measure CNT-coated PCM panel thermal conductivity using laser flash analysis (ASTM E1461) or guarded hot plate (ASTM C177). Target: 5–8 W/m·K. Verify anisotropy (in-plane vs. through-thickness).

Cycling Stability: Subject PCM samples to 1000 melt/solidify cycles (35–45 °C, 1 °C/min ramp). Re-measure latent heat and melting point by DSC. Acceptance: <10% degradation in latent heat; melting point shift <2 °C.

Leakage Test: Subject honeycomb-PCM panel to 100 cycles with 10% over-temperature (to 50 °C). Inspect for PCM leakage at seams and joints. Acceptance: no visible leakage; mass loss <1%.

## 7.2 System-Level Thermal Validation

Integrated pod-level testing validates the PCM buffer under realistic mission profiles:

Mission Cycle Simulation: Apply realistic power profile to QCL, MinION, and GPR simulators inside the sealed pod. Profile: 3× 15-min peak bursts (40 W excess) per hour, with 20-min idle between bursts. Monitor QCL/MinION junction temperatures, PCM surface temperatures, and shell exterior temperatures. Acceptance: QCL <45 °C, MinION <40 °C at all times; PCM does not fully melt.

Steady-State Comparison: Repeat test without PCM buffer (baseline sealed pod). Compare peak temperatures. Acceptance: PCM configuration reduces peak temperature by ≥8 °C.

Recharge Validation: After mission cycle, allow pod to idle at ambient for 30 min. Monitor PCM temperature and shell heat flux. Acceptance: PCM fully solidifies (temperature <35 °C) within 30 min, confirming recharge capability for next cycle.

IP54 Verification: After PCM integration, perform IEC 60529 IP54 test (dust + water spray). Verify no PCM contamination or moisture ingress. Acceptance: inner chamber passes IP54; PCM layer unaffected.

## 7.3 Validation Parameter Window

The following parameters require experimental determination to finalize the design:

| Parameter | Current Estimate | Validation Method |
| --- | --- | --- |
| PCM Thickness | 3–5 mm | Thermal test matrix: 2 mm, 3 mm, 4 mm, 5 mm, 6 mm |
| PCM Mass | ~0.3–0.5 kg | Mass optimization vs. heat capacity trade study |
| Thermal Conductivity (CNT coating) | 5–8 W/m·K | Laser flash analysis at multiple CNT loadings (3%, 5%, 8%, 10%) |
| Heat Capacity per Cycle | 60–80 kJ | Calorimetry + mission cycle simulation |
| Field Service Time | <5 min | Time-motion study with prototype panel replacement |
| IP54 Sealed Performance | Target: pass | IEC 60529 test after PCM integration |

# 8. RISK ASSESSMENT

| Risk | Likelihood | Impact | Mitigation |
| --- | --- | --- | --- |
| PCM degradation after >1000 cycles | Medium | High | DSC cycling test; select paraffin with stabilizers; salt hydrate with nucleation agents |
| PCM leakage from honeycomb containment | Low | High | Leakage test at 50 °C; aluminum foil sealing; redundant containment layer |
| Insufficient CNT thermal enhancement | Medium | Medium | Laser flash verification; optimize CNT loading and dispersion; alternative: graphite nanoplatelets |
| Supercooling preventing solidification | Medium | High | Nucleation agents in PCM formulation; seed crystals; verify solidification at 30–35 °C |
| PCM volume change cracking shell bond | Low | Medium | Flexible TIM layer; honeycomb cell expansion accommodation; strain relief pattern in bond line |
| High ambient preventing PCM solidification | Medium | Medium | Verify solidification at 40 °C ambient; TEC-assisted cooling during ground idle if needed |
| CNT delamination from thermal cycling | Low | Medium | Thermal cycling adhesion test; plasma surface treatment before CNT coating; flexible binder |

# 9. CROSS-DOMAIN INTEGRATION

This solution bridges thermal engineering, materials science, nanotechnology, and systems design:

Thermal Engineering: Phase-change heat transfer analysis (Stefan problem), transient thermal modeling (finite difference or FEM), and mission-cycle thermal management strategy. Time-separated heat storage and rejection decouples peak load from continuous cooling capacity.

Materials Science: PCM selection (organic paraffin vs. inorganic salt hydrate), thermal property characterization (DSC, TGA), and cycling stability testing. Honeycomb core material selection (aluminum vs. Nomex) for mass, conductivity, and compatibility trade-offs.

Nanotechnology: Carbon nanotube synthesis/selection (MWCNT diameter, length, purity), dispersion in epoxy matrix, percolation threshold modeling, and coating process development (spray, dip, or brush). Plasma surface treatment for CNT adhesion to honeycomb substrates.

Structural Engineering: Honeycomb panel design for PCM containment, structural bonding to aluminum ribs and carbon fiber shell, and accommodation of PCM volume change (up to 10%) without delamination or cracking.

Systems Engineering: Mass, power, and volume budgets reconciled with thermal performance requirements. TRIZ principles (#35 Parameter Change, #10 Prior Action) applied to create the time-separated thermal buffer. Field maintainability (<5 min panel swap) integrated into modular design. IP54 compliance maintained throughout.

# 10. REFERENCES

[1] Heat Dissipation Plate and Wind Turbine Generator Converter — Patent / Process Reference Document.

[2] Incropera, F.P. & DeWitt, D.P. 'Fundamentals of Heat and Mass Transfer.' 7th Ed., Wiley, 2011. (Phase change heat transfer)

[3] Zalba, B. et al. 'Review on Thermal Energy Storage with Phase Change: Materials, Heat Transfer Analysis and Applications.' Renewable and Sustainable Energy Reviews, 2003.

[4] Khodadadi, J.M. & Fan, L. 'Thermal Conductivity Enhancement of Phase Change Materials using Carbon Nanotubes.' Proceedings of IMECE, 2008.

[5] ASTM E794, 'Standard Test Method for Melting and Crystallization Temperatures by Thermal Analysis.'

[6] ASTM E1461, 'Standard Test Method for Thermal Diffusivity by the Flash Method.'

[7] IEC 60529:2013, 'Degrees of Protection Provided by Enclosures (IP Code).'

[8] TRIZ Journal — 'Principle #35: Parameter Change' and 'Principle #10: Prior Action.' (Innovation methodology reference)

# 11. APPENDIX: PHYSICAL CONTRACTIONS & TIME SEPARATION

## 11.1 Physical Contradictions Resolved

The PCM buffer resolves the fundamental physical contradiction of thermal management in sealed pods with limited cooling capacity:

Contradiction: Heat Rejection vs. Heat Storage: The system must reject heat to ambient (to prevent overheating) and store heat (to handle peaks exceeding continuous rejection capacity). These are mutually exclusive at any single instant — the shell cannot simultaneously reject heat and insulate the interior.

Resolution: Time Separation (TRIZ Principle #35 + #10): By separating heat rejection and heat storage in time, the contradiction is resolved. During peak operations, the PCM stores excess heat (Principle #10: Prior Action — the PCM is pre-positioned to absorb heat). During idle periods, the PCM releases stored heat to the shell (Principle #35: Parameter Change — the thermal state of the PCM changes from solid to liquid and back). The time dimension transforms an impossible simultaneous requirement into a feasible sequential process.

Parameter Change (Principle #35): The PCM changes its physical state (solid ↔ liquid) and effective thermal properties (low sensible heat → high latent heat) as a function of temperature. This parameter change is exploited to create a thermal 'switch' that automatically activates heat absorption at the melting point and deactivates it during solidification. No external control is required.

Prior Action (Principle #10): The PCM buffer is pre-positioned inside the shell before the mission begins. It is ready to absorb heat the instant the temperature rises, without activation delay. This prior action eliminates the need for real-time decision-making or active control systems.

## 11.2 Time Separation Strategy

The time separation is implemented through the mission cycle thermal profile:

Charge Phase (Heat In): Duration: 10–15 min per burst. PCM melts, absorbing 60–80 kJ. Temperature clamped at 35–40 °C. TEC operates at rated capacity; excess heat diverted to PCM.

Hold Phase (Heat Stored): Duration: 20–30 min between bursts. PCM remains molten, storing latent heat. Minimal heat generation; TEC maintains baseline cooling.

Discharge Phase (Heat Out): Duration: 20–30 min ground idle. PCM solidifies, releasing heat to shell. Shell radiates/convects to ambient. PCM recharged for next cycle.

Cycle Repetition: The 3-phase cycle repeats indefinitely as long as discharge time ≥ charge time. Mission planning ensures adequate idle/ground time between peak operations.

## 11.3 Parameter Changes from Baseline

The transition from a baseline sealed pod to a PCM-buffered pod involves the following parameter changes:

| Parameter | Baseline (Sealed Pod) | Modified (PCM Buffer) |
| --- | --- | --- |
| Peak Heat Handling | TEC saturation at >20 W excess; temperature spike | PCM absorbs 60–80 kJ; temperature clamped at ~40 °C |
| Thermal Response | Immediate temperature rise with load | Delayed temperature rise; flattened thermal profile |
| Added Mass | 0 kg | <0.5 kg (PCM + honeycomb + CNT coating) |
| Added Power | 0 W (baseline) | 0 W (passive — no power required) |
| Active Cooling Hardware | None (not feasible) | None (not required) |
| Field Serviceability | N/A | <5 min panel replacement |
| IP54 Compliance | Maintained | Maintained (sealed inner chamber) |

# DOCUMENT CONTROL

| Prepared By | Thermal Engineering & Materials Science Team |
| --- | --- |
| Reviewed By | Nanotechnology Specialist, Systems Engineer & QA Lead |
| Approved By | Chief Engineer |
| Distribution | Restricted — Engineering, QA, Manufacturing & Field Operations |
| Next Review Date | 2026-10-11 (90 days from issue) |